SECTION 07 4646

FIBER CEMENT SIDING

PART 1 - GENERAL

1.01	SECTION INCLUDES

A.	Wood-fiber cement siding.

B.	Soffit Panels

1.02	RELATED REQUIREMENTS

A.	Section 06 1000 - Rough Carpentry: Siding substrate.

B.	Section 07 9200 - Joint Sealants.

1.03	REFERENCE STANDARDS

A.	ASTM C1186 - Standard Specification for Flat Fiber Cement Sheets; 2008.

1.04	SUBMITTALS

A.	See Section 01 3000 - Administrative Requirements, for submittal procedures.

B.	Product Data:  Manufacturer's data sheets on each product to be used, including:

1.	Manufacturer's requirements for related materials to be installed by others.

2.	Preparation instructions and recommendations.

3.	Storage and handling requirements and recommendations.

4.	Installation methods, including nail patterns.

1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Company specializing in performing work of the type specified in this section with minimum 3 years of experience.

1.06	DELIVERY, STORAGE, AND HANDLING

A.	Store products under waterproof cover and elevated above grade, on a flat surface.

PART 2 - PRODUCTS

2.01	SIDING

A.	Panel Siding: Vertically oriented panels made of cement and cellulose fiber formed under high pressure, complying with ASTM C1186 Type A Grade II; with machined edges, for nail attachment.

1.	Texture:  Smooth.

2.	Length (Height):  96 inches, nominal.

3.	Width: 48 inches.

4.	Thickness: 5/16 inch, nominal.

5.	Finish:  Factory baked on color. Color chosen by Architect from manufacturer’s complete line of custom options.

6.	Warranty: 50 year limited; transferable.

7.	Panel Siding Manufacturers:

a.	CertainTeed Corporation:  www.certainteed.com.

b.	James Hardie Building Products, Inc:  www.jameshardie.com.

c.	Nichiha USA, Inc:  www.nichiha.com.

d.	Substitutions:  See Section 01 60 00 - Product Requirements.

B.	Soffit Panels:  Panels made of cement and cellulose fiber formed under high pressure with integral surface texture, complying with ASTM C1186 Type A Grade II; with machined edges, for nail attachment.

1.	Texture:  Smooth.

2.	Length:  96 inches, nominal.

3.	Width: 48 inches.

4.	Thickness: 5/16 inch, nominal.

5.	Finish:  Unfinished.

6.	Manufacturer:  Same as siding.

2.02	ACCESSORIES

A.	Trim:

1.	Trim Boards, Sheets, and One-Piece Corners: Smooth texture

a.	CertainTeed Restoration Millwork; www.certainteed.com.

B.	Fasteners:  Galvanized or corrosion resistant; length as required to penetrate minimum 1-1/4 inch.

C.	Joint Sealer:  As specified in Section 07 9200.

PART 3 - EXECUTION

3.01	PREPARATION

A.	Examine substrate and clean and repair as required to eliminate conditions that would be detrimental to proper installation.

B.	Do not begin until unacceptable conditions have been corrected.

C.	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

3.02	INSTALLATION

A.	Install in accordance with manufacturer's instructions and recommendations.

1.	Read warranty and comply with all terms necessary to maintain warranty coverage.

2.	Use trim details indicated on drawings.

3.	Touch up all field cut edges before installing.

4.	Pre-drill nail holes if necessary to prevent breakage.

B.	Over Wood and Wood-Composite Sheathing:  Fasten siding through sheathing into studs.

C.	Allow space between both ends of siding panels that butt against trim for thermal movement; seal joint between panel and trim with exterior grade sealant.

D.	Joints in Vertical Siding:  Install Z-flashing in horizontal joints between successive courses of vertical siding.

E.	Do not install siding less than 6 inches from surface of ground nor closer than 1 inch to roofs, patios, porches, and other surfaces where water may collect.

F.	After installation, seal all joints except lap joints of lap siding.  Seal around all penetrations.  Paint all exposed cut edges.

G.	Finish Painting:  Specified in Section 09 9100.

3.03	PROTECTION

A.	Protect installed products until completion of project.

B.	Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION 07 4646