SECTION 07 9200

JOINT SEALANTS

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Urethane joint sealants.

          - Silicone joint sealants

        - Related Sections:

          - Section 04 2000 "Unit Masonry" for masonry control and expansion joint fillers and gaskets.

      - ACTION SUBMITTALS

        - Product Data:  For each joint-sealant product indicated.

        - Joint-Sealant Schedule:  Include the following information:

          - Joint-sealant application, joint location, and designation.

          - Joint-sealant manufacturer and product name.

          - Joint-sealant formulation.

          - Joint-sealant color.

      - INFORMATIONAL SUBMITTALS

        - Qualification Data:  For qualified Installer.

        - Product Certificates:  For each kind of joint sealant and accessory, from manufacturer.

        - Sealant, Waterproofing, and Restoration Institute (SWRI) Validation Certificate:  For each sealant specified to be validated by SWRI's Sealant Validation Program.

        - Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, indicating that sealants comply with requirements.

        - Warranties:  Sample of special warranties.

      - QUALITY ASSURANCE

        - Installer Qualifications:  Manufacturer's authorized representative who is trained and approved for installation of units required for this Project.

        - Source Limitations: Obtain each kind of joint sealant from single source from single manufacturer.

        - Pre-installation Conference:  Conduct conference at Project site.

      - PROJECT CONDITIONS

        - Do not proceed with installation of joint sealants under the following conditions:

          - When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer or are below 40 deg F (5 deg C).

          - When joint substrates are wet.

          - Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

          - Where contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

      - WARRANTY

        - Special Installer's Warranty:  Manufacturer's standard form in which Installer agrees to repair or replace joint sealants that do not comply with performance and other requirements specified in this Section within specified warranty period.

          - Warranty Period:  Two years from date of Substantial Completion.

        - Special Manufacturer's Warranty: Manufacturer's standard form in which joint-sealant manufacturer agrees to furnish joint sealants to repair or replace those that do not comply with performance and other requirements specified in this Section within specified warranty period.

          - Warranty Period: Five years from date of Substantial Completion.

        - Special warranties specified in this article exclude deterioration or failure of joint sealants from the following:

          - Movement of the structure caused by structural settlement or errors attributable to design or construction resulting in stresses on the sealant exceeding sealant manufacturer's written specifications for sealant elongation and compression.

          - Disintegration of joint substrates from natural causes exceeding design specifications.

          - Mechanical damage caused by individuals, tools, or other outside agents.

          - Changes in sealant appearance caused by accumulation of dirt or other atmospheric contaminants.

- PRODUCTS

      - MATERIALS, GENERAL

        - Compatibility:  Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint-sealant manufacturer, based on testing and field experience.

        - Colors of Exposed Joint Sealants:  As selected by Architect from manufacturer's full range.

      - SILICONE JOINT SEALANTS

        - Single-Component, Nonsag, Neutral-Curing Silicone Joint Sealant:  ASTM C 920, Type M, Grade NS, Class 50, for Use NT.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

          - Basis of Design:  Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

            - Tremco Incorporated; Spectrem 4-TS.

        - Mildew-Resistant, Single-Component, Nonsag, Mopisture-Curing Silicone Joint Sealant:  ASTM C 920, Type S, Grade NS, Class 25, for Use NT.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

          - Basis of Design:  Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

            - Tremco Incorporated; Tremsil 200.

      - URETHANE JOINT SEALANTS

        - Multicomponent, Nonsag, Urethane Joint Sealant:  ASTM C 920, Type M, Grade NS, Class 50, for Use NT.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Section 016000 "Product Requirements."

          - Basis of Design:  Subject to compliance with requirements, available products that may be incorporated into the Work include, but are not limited to, the following:

            - Tremco Incorporated; Dymeric 240 FC.

      - JOINT SEALANT BACKING

        - General:  Provide sealant backings of material that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

        - Cylindrical Sealant Backings: ASTM C 1330, Type C (closed-cell material with a surface skin), Type O (open-cell material), Type B (bicellular material with a surface skin),  or any of the preceding types, as approved in writing by joint-sealant manufacturer for joint application indicated, and of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance.

        - Bond-Breaker Tape: Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint.  Provide self-adhesive tape where applicable.

      - MISCELLANEOUS MATERIALS

        - Primer:  Material recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

        - Cleaners for Nonporous Surfaces:  Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants to joint substrates.

        - Masking Tape:  Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

- EXECUTION

      - EXAMINATION

        - Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Surface Cleaning of Joints: Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions and the following requirements:

          - Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, paints (except for permanent, protective coatings tested and approved for sealant adhesion and compatibility by sealant manufacturer), oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

          - Clean porous joint substrate surfaces by brushing, grinding, mechanical abrading, or a combination of these methods to produce a clean, sound substrate capable of developing optimum bond with joint sealants.  Remove loose particles remaining after cleaning operations above by vacuuming or blowing out joints with oil-free compressed air.  Porous joint substrates include the following:

            - Concrete.

            - Masonry.

          - Remove laitance and form-release agents from concrete.

          - Clean nonporous joint substrate surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues capable of interfering with adhesion of joint sealants.  Nonporous joint substrates include the following:

            - Metal.

            - Porcelain enamel.

        - Joint Priming:  Prime joint substrates where recommended by joint-sealant manufacturer or as indicated by preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint-sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

        - Masking Tape:  Use masking tape where required to prevent contact of sealant or primer with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears.  Remove tape immediately after tooling without disturbing joint seal.

      - INSTALLATION OF JOINT SEALANTS

        - General:  Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

        - Sealant Installation Standard:  Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

        - Install sealant backings of kind indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

          - Do not leave gaps between ends of sealant backings.

          - Do not stretch, twist, puncture, or tear sealant backings.

          - Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

        - Install bond-breaker tape behind sealants where sealant backings are not used between sealants and backs of joints.

        - Install sealants using proven techniques that comply with the following and at the same time backings are installed:

          - Place sealants so they directly contact and fully wet joint substrates.

          - Completely fill recesses in each joint configuration.

          - Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

        - Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified in subparagraphs below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

          - Remove excess sealant from surfaces adjacent to joints.

          - Use tooling agents that are approved in writing by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

          - Provide concave joint profile per Figure 8A in ASTM C 1193, unless otherwise indicated.

          - Provide flush joint profile where indicated per Figure 8B in ASTM C 1193.

          - Provide recessed joint configuration of recess depth and at locations indicated per Figure 8C in ASTM C 1193.

            - Use masking tape to protect surfaces adjacent to recessed tooled joints.

      - CLEANING

        - Clean off excess sealant or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of joint sealants and of products in which joints occur.

      - PROTECTION

        - Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from original work.

      - JOINT-SEALANT SCHEDULE

        - Joint-Sealant Application: Exterior joints in vertical surfaces.

          - Joint Locations:

            - Joints between different materials.

            - Perimeter joints between materials listed above and frames of doors.

            - Other joints as indicated.

          - Silicone Joint Sealant: Single-Component, Nonsag, Neutral-Curing.

          - Joint-Sealant Color:  As selected by Architect from manufacturer's full range of colors.

        - Joint-Sealant Application:  Interior joints in vertical surfaces.

          - Joint Locations:

            - Perimeter joints of exterior openings.

            - Vertical joints on exposed surfaces of interior unit masonry walls and partitions.

            - Perimeter joints between interior wall surfaces and frames of interior doors.

          - Urethane Joint Sealant: Multi-component, Nonsag,

          - Joint-Sealant Color:  As selected by Architect from manufacturer's full range of colors.

        - Joint-Sealant Application: Mildew-resistant interior joints in vertical surfaces.

          - Joint Sealant Location:

            - Joints between plumbing fixtures and adjoining walls, floors, and counters.

            - Other joints as indicated.

          - Silicone Joint Sealant:  Mildew resistant, single component, nonsag, moisture curing.

          - Joint-Sealant Color:  As selected by Architect from manufacturer's full range of colors.

END OF SECTION 07 9200