SECTION 09 9100

- PAINTING

- GENERAL

  - SECTION INCLUDES

    - Interior Primer.

    - Interior Paint.

    - Exterior Primer.

    - Exterior Paint.

    - Wall Preparation.

  - RELATED SECTIONS

    - Section 09 2000 - Gypsum Board: Preparation of interior wall sheathing to receive finishes.

  - REFERENCES

    - 40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings; U.S. Environmental Protection Agency; current edition.

  - DEFINITIONS

    - Paints are available in a wide range of sheens or glosses, as measured by a gloss meter from a 60 degree angle from vertical, as a percentage of the amount of light that is reflected.  The following terms are used to describe the gloss of our products.

      - Flat - Less than 5 units.

      - Matte - 0 - 10 units.

      - Eggshell - 10 - 25 units.

      - Satin - 20 - 35 units.

      - Semi-Gloss - 35 - 70 units.

      - Gloss - 70 - 85 units.

  - SUBMITTALS

    - Submit under provisions of Section 01 3000.

    - Product Data:  Provide a complete list of all products to be used, with the following information for each:

      - Manufacturer's name, product name and/or catalog number, and general product category.

      - Cross-reference to specified paint system(s) that the product is to be used in; include description of each system.

    - Samples:  Submit three paper samples, 5 inches by 7 inches (127mm x 178mm) in size, illustrating selected colors for each color and system selected with specified coats cascaded.

    - Manufacturer's Instructions:  Indicate special surface preparation procedures.

    - Maintenance Data:  Submit data on cleaning, touch-up, and repair of painted and coated surfaces.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: a single manufacturer with a minimum of ten (10) years experience will supply all primary products specified in this section.

    - Installer Qualifications: All products listed in this section are to be installed by a single installer with a minimum of five (5) years demonstrated experience in installing products of the same type and scope as specified.

  - DELIVERY, STORAGE, AND HANDLING

    - Store products in manufacturer's unopened packaging until ready for installation.

    - Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

    - Disposal:

      - Never pour leftover coating down any sink or drain.  Use up material on the job or seal can and store safely for future use.

      - Do not incinerate closed containers.

      - For specific disposal or recycle guidelines, contact the local waste management agency or district. Recycle whenever possible.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

  - WARRANTY

    - At project closeout, provide to the Owner or owner's representative an executed copy of the Manufacturer's standard form outlining the terms and conditions of and any exclusions to their Limited Warranty against Manufacturing Defect.

  - EXTRA MATERIALS

    - At project closeout, supply the Owner or owner's representative one gallon of each product for touch-up purposes.

    - At project closeout, provide the color mixture name and code to the Owner or owner's representative for accurate future color matching.

- PRODUCTS

  - MANUFACTURERS

    - Basis of Design:

      - Benjamin Moore & Co., which is located at: 101 Paragon Drive, Montvale, NJ 07645; Toll Free Tel: 866-708-9181; Tel: 201-573-9600; Email: info@benjaminmoore.com; Web: www.benjaminmoore.com

      - Complementary Coatings Corporation; Main Office - Factory Customer Service; 101 Paragon Drive · Monvtale , NJ 07645; Phone : (800) 225-5554; Fax : (888) 248-2143; www.insl-x.com.

      - Local Contact: Vicki Persons; 651-829-0783; vicki.persons@benjaminmoore.com.

    - Other acceptable manufacturers include, but are not necessarily limited to:

      - Devoe; .www.devoe.com.

      - Diamond Vogel Paint Manufacturing; www.diamondvogel.com

      - Hirshfields Inc.; www.hirshfields.com.

      - Pratt and Lambret Paints; www.prattandlambert.com

      - Sherwin Williams; www.sherwin-williams.com.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.

  - MATERIALS - GENERAL

    - Volatile Organic Compound (VOC) Content:

      - Provide coatings that comply with the most stringent requirements specified in the following:

        - 40 CFR 59, Subpart D--National Volatile Organic Compound Emission Standards for Architectural Coatings.

        - Determination of VOC Content:  Testing and calculation in accordance with 40 CFR 59, Subpart D (EPA Method 24), exclusive of colorants added to a tint base and water added at project site; or other method acceptable to authorities having jurisdiction.

    - Compatibility: Provide materials that are compatible with one another and the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.

  - MIXING AND TINTING

    - Except where specifically noted in this section, all paint shall be ready-mixed and pre-tinted.  Agitate all paint prior to and during application to ensure uniform color, gloss, and consistency.

    - Thinner addition shall not exceed manufacturer's printed recommendations.  Do not use kerosene or other organic solvents to thin water-based paints.

    - Where paint is to be sprayed, thin according to manufacturer's current guidelines.

  - EXTERIOR APPLICATIONS

    - Fiber Cement Board

      - Primer: One coat Benjamin Moore Super Spec® Masonry Int./Ext. Acrylic High Build Masonry Primer Primer #N068.

      - Finish: Two coats Benjamin Moore Ultra Spec Exterior Flat Finish #N447.

    - Fiber Cement Board Trim

      - Primer: One coat Benjamin Moore Super Spec® Masonry Int./Ext. Acrylic High Build Masonry Primer #N068.

      - Finish: Two coats Benjamin Moore Ultra Spec Exterior Satin Finish #N448.

  - INTERIOR APPLICATIONS

    - Concrete Masonry Units:

      - Primer: One coat Corotech Epoxy Block Filler # V163-01

      - Finish:	 One coat Corotech Waterborne Amine Epoxy #V440

    - Wood:

      - Primer: One coat Benjamin Moore Fresh Start All Purpose Int/Ext. Primer #N023

      - Finish: Two coats Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish #N539

    - Ferrous Metal:

** NOTE TO SPECIFIER **  Select resin type from the following two options.  Of the included subparagraphs, retain only material(s) required on this project.

      - Two coats Benjamin Moore Super Spec DTM Acrylic Semi-Gloss #P29

    - Galvanized Metal:

      - Two coats Benjamin Moore Super Spec DTM Acrylic Semi-gloss #P29.

** NOTE TO SPECIFIER **  Select material required on this project.  Delete four of the next five paragraphs.

    - Gypsum Board:

** NOTE TO SPECIFIER **  Select resin type from the following two options.  Of the included subparagraphs, retain only material(s) required on this project.

      - Primer: One coat Benjamin Moore Fresh Start Superior Int/Ext. Primer #N023

      - Finish: Two coats Ultra Spec 500 Semi-gloss Finish #N539.

** NOTE TO SPECIFIER **  Retain the next Article only if Floor Coatings are required.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly prepared.

    - Ensure that surfaces to receive paint are dry immediately prior to application.

    - Ensure that moisture-retaining substrates to receive paint have moisture content within tolerances allowed by coating manufacturer.  Where exceeding the following values, promptly notify Architect and obtain direction before beginning work.

      - Concrete and Masonry: 13 percent. Allow new concrete to cure a minimum of 28 days.

      - Exterior Wood: 17 percent.

      - Interior Wood: 15 percent.

      - Interior Finish Detail Woodwork, Including Trim, and Casework: 10 percent.

      - Gypsum: 15 percent.

    - Examine surfaces to receive coatings for surface imperfections and contaminants that could impair performance or appearance of coatings, including but not limited to, loose primer, rust, scale, oil, grease, mildew, algae, or fungus, stains or marks, cracks, indentations, or abrasions.

    - CMU surfaces shall be sound, dry, clean and free of oil, grease, dirt, mildew, mill scale, loose and flaking paint and other surface contaminants.

      - Allow masonry surfaces to cure a minimum of 30 days before painting. Acid etch or abrasive blast slick, glazed concrete or concrete with laitance. For acid etching, follow manufacturer’s directions and safety instructions. Rinse thoroughly and allow to dry.

    - Correct conditions that could impair performance or appearance of coatings in accordance with specified surface preparation procedures before proceeding with coating application.

  - PREPARATION - GENERAL

    - Clean surfaces thoroughly prior to coating application.

    - Do not start work until surfaces to be finished are in proper condition to produce finished surfaces of uniform, satisfactory appearance.

    - Stains and Marks: Remove completely, if possible, using materials and methods recommended by coating manufacturer; cover stains and marks which cannot be completely removed with isolating primer or sealer recommended by coating manufacturer to prevent bleed-through.

    - Remove Mildew, Algae, and Fungus using materials and methods recommended by coating manufacturer.

    - Remove dust and loose particulate matter from surfaces to receive coatings immediately prior to coating application.

    - Remove or protect adjacent hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items not indicated to receive coatings.

    - Move or protect equipment and fixtures adjacent to surfaces indicated to receive coatings to allow application of coatings.

    - Protect adjacent surfaces not indicated to receive coatings.

    - Prepare surfaces in accordance with manufacturer's instructions for specified coatings and indicated materials, using only methods and materials recommended by coating manufacturer.

  - SURFACE PREPARATION

    - Concrete Masonry: Clean surfaces free of loose particles, sand, efflorescence, laitance, form oil, curing compounds, and other substances which could impair coating performance or appearance.

    - Gypsum Board: Repair cracks, holes and other surface defects with joint compound to produce surface flush with adjacent surfaces.

    - Metals - Ferrous, Unprimed: Remove rust or scale, if present, by wire brush cleaning, power tool cleaning, or sandblast cleaning; remove grease, oil, and other contaminants which could impair coating performance or appearance by solvent cleaning, with phosphoric-acid solution cleaning of welds, bolts and nuts; spot-prime repaired welds with specified primer.

    - Metals - Ferrous, Shop-Primed: Remove loose primer and rust, if present, by scraping and sanding, feathering edges of cleaned areas to produce uniform flat surface; solvent-clean surfaces and spot-prime bare metal with specified primer, feathering edges to produce uniform flat surface.

    - Galvanized Metals – Thoroughly clean surfaces with Super Spec HP® Oil & Grease Emulsifier (P83) to remove contaminants. Dull new shiny non-ferrous metal surfaces subject to abrasion with very fine sandpaper.

    - Wood:

      - Seal knots, pitch streaks, and sap areas with sealer recommended by coating manufacturer; fill nail recesses and cracks with filler recommended by coating manufacturer; sand surfaces smooth.

      - Apply primer coat to back of wood trim and paneling.

  - APPLICATION - GENERAL

    - Apply each coat to uniform coating thickness in accordance with manufacturer's instructions, not exceeding manufacturer's specified maximum spread rate for indicated surface; thins, brush marks, roller marks, orange-peel, or other application imperfections are not permitted.

    - Allow manufacturer's specified drying time, and ensure correct coating adhesion, for each coat before applying next coat.

    - Inspect each coat before applying next coat; touch-up surface imperfections with coating material, feathering, and sanding if required; touch-up areas to achieve flat, uniform surface without surface defects visible from 5 feet (1.5 m).

    - Remove dust and other foreign materials from substrate immediately prior to applying each coat.

    - Where paint application abuts other materials or other coating color, terminate coating with a clean sharp termination line without coating overlap.

    - Where color changes occur between adjoining spaces, through framed openings that are of same color as adjoining surfaces, change color at outside stop corner nearest to face of closed door.

    - Re-prepare and re-coat unsatisfactory finishes; refinish entire area to corners or other natural terminations.

  - CLEANING

    - Clean excess coating materials, and coating materials deposited on surfaces not indicated to receive coatings, as construction activities of this section progress; do not allow to dry.

    - Re-install hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items that have been removed to protect from contact with coatings.

    - Reconnect equipment adjacent to surfaces indicated to receive coatings.

    - Relocate to original position equipment and fixtures that have been moved to allow application of coatings.

    - Remove protective materials.

  - PROTECTION

    - Protect completed coating applications from damage by subsequent construction activities.

    - Repair to Architect's acceptance coatings damaged by subsequent construction activities. Where repairs cannot be made to Architect's acceptance, re-apply finish coating to nearest adjacent change of surface plane, in both horizontal and vertical directions.

- END OF SECTION 09 9100